Technical data sheet:

Mohawk Via Felt: expressive colour and texture

Mohawk Via Felt offers a distinctive felt-marked texture reminiscent of that achieved by the traditional wool felts used in the paper-making process since the 19th century.

Available in white, natural, fibred and deep shades, this sophisticated finish brings another dimension to any printed project.

- Specified by the US print and creative communities for over 25 years

- Delivering Mohawk quality and performance at a budget-friendly price point

- Manufactured acid free to meet ANSI standards for archival permanence

- Excellent on-press performance – uniform, stable and consistent

- Available with i-tone surface technology for HP Indigo printing

- Manufactured with wind energy, produced carbon neutral and FSC certified

| FINISH | SHADE | GSM | CALIPER [µ] | OPACITY | TAPPI | CIE | PPI |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Felt | Pure White | 100 | 160 | 93 | 96 | 143 | 334 |
|  |  | 120 | 178 | 94 | 96 | 143 | 286 |
|  |  | 220 | 305 | 98 | 96 | 143 | 168 |
|  |  | 270 | 381 | 98 | 96 | 143 | 134 |
|  |  | 300 | 422 | 98 | 96 | 143 | 120 |
|  |  | 350 | 445 | 99 | 96 | 143 | 114 |
|  | Natural | 100 | 160 | 93 |  |  | 334 |
|  |  | 120 | 178 | 94 |  |  | 286 |
|  |  | 220 | 305 | 98 |  |  | 168 |
|  |  | 270 | 381 | 99 |  |  | 134 |
|  |  | 350 | 445 | 99 |  |  | 114 |
|  | Flax | 100 | 160 |  |  |  | 318 |
|  |  | 220 | 305 |  |  |  | 168 |
|  | Jute | 100 | 160 |  |  |  | 318 |
|  |  | 220 | 305 |  |  |  | 168 |
|  | Ginger | 300 | 410 |  |  |  | 124 |
|  | Coco | 300 | 410 |  |  |  | 124 |
|  | Black | 350 | 479 |  |  |  | 106 |